## Slide 1: Superconducting Magnets 2
GianLuca Sabbi
Lawrence Berkeley National Laboratory
IAS 2023
July 16-17, 2023

## Slide 2: Next HEP collider: HL-LHC
Goal: 10x integrated luminosity enabled by new IR magnets
first application of Nb3Sn technology in a high energy collider

## Slide 3: IR Quadrupole Parameter Optimization
Nb3Sn technology enables HL-LHC luminosity target

## Slide 4: Nb3Sn Technology
Brittle material:
Severe damage in cabling/winding
React coils after winding
New coil materials (insulation, parts)
Cheggour
Sci Rep 9 (2019)
Sensitivity to stress/strain:
Epoxy impregnation
New mechanical designs
Winding
Post-reaction
Epoxy-impregnation
Reaction

## Slide 5: Aluminum-shell based support structure
Mechanical design of Nb3Sn magnets needs to satisfy stringent constraints
  Full support without exceeding stress limits (150-200 MPa cold)
Selected structure is based on aluminum shell over iron yoke, preloaded with pressurized bladders and interference keys
  Minimize and precisely control warm pre-load
  Increase to full pre-load during cool-down, avoiding overshoot
S. Caspi, P. Ferracin et al.

## Slide 6
HL-LHC IR Quad production is underway
Common design for US (Q1/Q3) and CERN (Q2a/b) Quadrupoles except for different length (4.2+4.2 m vs 7.15 m)
Nb3Sn strand
Beam screen w/tungsten absorbers
Cross-section of cold mass and cryostat
4 m long
Nb3Sn
coil

## Slide 7
Field Quality Table
Reference: Hi Lumi LHC Work Package 3 - Magnets for Insertion Regions https://espace.cern.ch/HiLumi/WP3/SitePages/Home.aspx

## Slide 8
Field Error Measurements and Analysis
USPAS 2006 - A. Jan, BNL
Conductor Magnetization
Magnetization measurement
Iron saturation
Integrated Harmonics
at nominal field
S. Izquierdo Bermudez, X. Wang, A. Ben Yahia,
M. Sumption et al.

## Slide 9
Quench Protection with CLIQ
E. Ravaioli, CERN
Power is deposited by inter-filament coupling currents induced by the rapid current oscillations

## Slide 10
Test Instrumentation
Ultrasonic transducer
Acoustic sensor
M. Marchevsky, USPAS 2022
Quench antenna
New diagnostics are being developed to complement the traditional approach based on voltage taps

## Slide 11
190
MPa
0 MPa
Coil Stress @ B0 = 16 T
Magnetic Field @ B0 = 16 T
0 MPa
190
MPa
HD2 Design:
High Je (no spacers/structure in coil)
  Efficient design for small aperture
Only two co-wound layers/pole
  Optimize performance and cost
Concentrates stress in low-field region
Internal bore support (vs. Roman arch)
Flared ends (vs. saddle ends)
Winding
Pole
Central support tube
(tested with/without)
Bore structural support
200 MPa (0T)
200 MPa (0T)
36 mm
EM force
Block-coil High Field Dipole Design

## Slide 12
Twin-Aperture Collider Dipoles
Short sample performance | Iss |  | B1ss | 
Temperature | 4.5K | 1.9K | 4.5K | 1.9K
Single aperture (HD2) | 18.0 | 20.1 | 15.52 | 17.15
Double aperture (2HD) | 17.8 | 19.7 | 15.49 | 17.12
Asymmetric coil design for smaller spacing between apertures
Horizontal layout has good magnetic and mechanical efficiency

## Slide 13
Past improvements of Nb3Sn Jc
HEP conductor development program resulted in +3T field potential (4.5K)
Achieved performance consistent with improvements in conductor properties
Optimal design choices driven by accelerator requirements and production cost
Bore field to peak field ratios:
  D20 : 0.98
  HD2: 0.95
  HD1: 1.06
  RD3: 0.99

## Slide 14: Potential for further improvements
Principle: increase of Nb3Sn pinning force at high field through grain refinement
Promising results in short samples (X. Xu et al, Appl. Phys. Lett. 104 082602):
Extrapolation to HD2 & 13 nm grain size (G. Sabbi et al., IEEE-TAS 25 (3) 4001407):
HD2 cross-section
Jc(12 T, 4.2K): from
3.5 kA/mm2 @ 100+ nm (e.g. best HD2 wire) to
9.6 kA/mm2 @ ~35 nm
B0>19T
@ 4.5K

## Slide 15
High Temperature Superconductors (HTS)
In-depth analysis & optimization
Conductor properties
Fabrication technology
Material characterization
Modeling and diagnostics
Technology foundation:
Conductor properties
Fabrication methods
Design concepts, tools
Performance demonstration in simple configurations
Full qualification in
accelerator configurations
System integration
Bi-2212
YBCO
Nb3Sn
NbTi

## Slide 16
Accelerator-type coils with Bi-2212
Significant Jc improvements with new high pressure heat treatment and powers
RC-06 results (0.8 mm strand, 17-strand Rutherford cable, 2-layer, 6-turn/layer):
  Je - 1365 A/mm2 at 15 T (2xFCC spec); 1000 A/mm2 at 27 T (1.3 GHz NMR)
Two larger 11-turn coils (RC7-8) generated 4.5 T field in a shell-based structure
2x6 turn coil
2x11 turn coil
Zhang et al. SuST, 31 (2018) 105009
Jiang et al., IEEE TAS, 29 (2019), 6400405
Shen et al., arXiv preprint arXiv:1808.02864

## Slide 17
REBCO tapes: the high field frontier
REBCO tapes provide by far the best current densities at the highest field
Enabling impressive progress in hybrid LTS/HTS superconducting solenoids
  Highest field all superconducting user facility (32 T) – 12/2017
  All-SC test achieves highest magnetic field on record (45.5 T) – 2/2019
  First commercial 1.2 GHz NMR (28.2T) system by Bruker – 8/2019
D. Larbalestier, NHMFL
M. Bird, NHMFL

## Slide 18
Key technology: high current HS cables
Goal: develop multi-kA HTS cables with low degradation from cabling, bending and stress, and low AC losses
REBCO is strongly preferred to Bi-2212 in large systems due to lower projected cost and avoiding the challenging reaction
Conductor on Round Core (CORC)
Twisted stack
Robel cable
ITER CICC
(Nb3Sn)
REBCO
tape

## Slide 19: Cable-in-groove
Concept: place individual turns in grooved formers
Goals:
  More flexibility in the winding pattern, cable design, and coil grading
  Internal structure to protect the conductor from force accumulation
Issues to be addressed for application to high field magnets
  Magnetic: engineering current density, quench propagation
  Mechanical: pre-load transfer, or capability to operate without pre-load
  Tooling/processes for reaction and impregnation; reliable insulation
  Field quality: tolerances for cable insertion, module assembly/alignment
Cosq
Racetrack
Helical Winding

## Slide 20: CORC Wires in Helical Windings
Two-layer dipole: 1.2 T at 4.2 K
X. Wang et al. SuST (2018) 075002
Four-layer dipole: 2.9 T at 4.2 K
Basic concept: superposition of tilted solenoids to generate a dipole field (Meyer, NIM 1970)
Windings can be further modulated to generate higher order multipoles and control the field in curved or tapered geometries

## Slide 21
Accelerator-type coils for ECR sources
gas
ions
sextupole
solenoid
Ion current scales as square of microwave frequency
Confinement field scales linearly with frequency

## Slide 22
Very favorable performance (current) scaling with square of frequency/field
Main challenge is the sextupole coil fabrication and mechanical support
Requires lower current (<1-2 kA) than typical in large accelerator applications
  Single wire or small Rutherford cable – but both require many layers
Shell based structure is directly applicable with additional challenges
  Asymmetric force distribution and sextupole-solenoid integration
45-56 GHz ECR magnets with Nb3Sn
Conductor options
Magnetic and mechanical design
Energy extraction vs. CLIQ
45 GHz Design by IMP and LBNL
Single wire
(baseline)
6-strand mini-cable
(alternative)

## Slide 23: Medical applications: compact cyclotrons
Strong reduction of cyclotron size and weight at higher field (1/B3)
  Of particular benefit for installations in medical facilities
Significant progress in compact (synchro)cyclotrons for proton therapy
  Up to 7 T with NbTi and 9 T with Nb3Sn
Higher field is possible from a magnet perspective, but there are challenges in beam physics and system integration
  Potential opportunities in carbon therapy
Consider potential benefits from “high field” technology in specific sub-systems: gantries, cryogenics, flux return coils etc.

## Slide 24
Concluding Remarks
Superconducting Accelerator Magnets are a very broad subject combining different disciplines from material science to magnetics, mechanical engineering, cryogenics, power electronics and related instrumentation and diagnostics
Solid technological basis and exciting developments with many technical challenges, both near term and long term
Progress in high field magnets requires a convergence of technical feasibility, performance benefits for the application and critical mass to support the R&D
Several new technologies are reaching maturity, offering opportunities for new application