## Slide 1: Basic principles of RF Superconductivity
Tobias Junginger

## Slide 2: Particle Acceleration with cavities
H
E
beam direction
Particle bunch
H
E
beam direction
Particle bunch
H
E
beam direction
Particle bunch
1. Acceleration with radiofrequency cavities requires synchronization of particles and RF field. Outside of the cavity the approaching particle bunch does not experience the RF field
2. The particle bunch enters the cavity. The electric field is pointing in the direction of the beam axis  The particle is accelerated
3. The particle bunch leaves the cavity. The field direction has changed again
Free space:
Ohm‘s law: =σE
In this lecture we will address these questions:
Superconductivity means no resistance. Why can’t we reduce the losses zero?
Why is niobium the material choice which requires costly helium cooling?
What are the fundamental and technical limitations of niobium SRF cavities?
  Highest Energy Gain  Maximum Accelerating Gradient?
  Lowest cryogenic losses  Maximum Quality Factor?
What are possible future materials and what are the challenges?
Cavities are used to accelerate particles by an alternating electric field
An oscillating electric field causes an oscillating magnetic field
The cavity confines the electromagnetic fields by surface shielding currents
These currents create losses (heating), which can be reduced by using superconducting materials

## Slide 3: Performance of SRF cavities
There are two parameters which define the performance of an SRF cavity: Quality factor and the accelerating gradient
B
E
The quality factor:
Q0 =G/RS=U/Ploss
G: Geometry factor
The accelerating gradient can be limited by the peak surface electric field (field emission) or the peak surface magnetic field (quench)
Accelerating Gradient Eacc ∝ Bpeak
There are two ways to increase performance: Shape and material optimization
In this lecture the focus is on material optimization. What are the intrinsic limitations to Rs and Bpeak
Shape optimization and extrinsic limitations, i.e Multipacting, field emission and thermal breakdown are covered in Bob’s lecture
Quality FactorQ0 =G/RS=U/Ploss

## Slide 4: Surface treatments for State of the art SRF cavities
SRF is highly efficient but complex technology
Supercurrents only flow within a few tens of nanometres
  Performance is very sensitive to near surface material properties which can be engineered by heat treatments in vacuum or low pressure gas atmosphere
Maximum quality factor and accelerating gradient depend on surface treatment but also on RF frequency, cavity shape (surface field configuration), ambient magnetic flux in a correlated and not fully understood way

## Slide 5: Superconducting Materials

## Slide 6: Outline
Quick recap of London theory and demonstration of the Meissner effect
Surface Resistance
  Electrodynamics of normal conductors
    Normal and anomalous skin effect
  Electrodynamics of superconductors
    Surface impedance of superconductors in the two fluid model and the BCS theory
    Residual resistance
    Field dependence of surface resistance
Maximum RF field
  DC critical fields, Hc, Hc1, Hc2, Hsh
  Critical field under RF
Materials for SRF
  Why niobium
  Materials beyond niobium
  Multilayers

## Slide 7: Outline
Quick recap of London theory and demonstration of the Meissner effect
Surface Resistance
  Electrodynamics of normal conductors
    Normal and anomalous skin effect
  Electrodynamics of superconductors
    Surface impedance of superconductors in the two fluid model and the BCS theory
    Residual resistance
    Field dependence of surface resistance
Maximum RF field
  DC critical fields, Hc, Hc1, Hc2, Hsh
  Critical field under RF
Materials for SRF
  Why niobium
  Materials beyond niobium
  Multilayers

## Slide 8: Overview of theories
London Theory
  Based on Maxwell´s equations. Phenomenological theory that can describe zero resistance and the Meissner effect
  Best applicable to Type-II superconductors
Ginzburg Landau Theory
  Can describe non-local effects
  Applicable to Type-I and II superconductors
BCS Theory
  First microscopic theory of superconductivity
  Published 46 years after the discovery of superconductivity

## Slide 9: The London Theory
Assume an electron which is freely accelerated by an electric field
F
Lorentz force acting on the particle:
J
Definition of the current density
E
E=0
0
1st London Equation
The goal is to obtain a differential equation for B
To explain the Meissner effect we want to derive an equation that relates J to B
Maxwell equation:

## Slide 10: The London Theory
0
Maxwell equation
0
Let us check which solution is physically meaningful
2. B(x)
2 possible solutions:
with
London penetration depth
B0
B(x)
Ampere´s law relates the current density J and the magnetic flux density B

## Slide 11: Perfect Conductor
2. B(x)
This is not what we observe in superconductors
Consider a conductor which fulfills these solutions when cooled below its critical temperature
0

## Slide 12: Superconductor - Meissner Effect
2. B(x)
Superconductivity is a phase transition
The final state does not depend on the order of cooling and applying field
The constant solution is not physically meaningful

## Slide 13: London Theory and Meissner Effect
0
2. B(x)
Only exponential decaying fields are observed
To explain the Meissner effect the Londons postulated:
Finally we have derived the two London equations:
E
Zero Resistance
Meissner Effect

## Slide 14: Pippards extension of London´s Theory
Pippard found that λL depends on the purity of the material and therefore on the electron mean free path l
He introduced of the new parameter coherence length ξ in analogy to the anomalous skin effect in normal conductors
Pippard introduced ξ as a phenomenological parameter. Later explained by the microscopic BCS theory
Non-local relation between current density and vector potential:
A.B Pippard - Proceedings of the Royal Society of London. A Vol. 216, No. 1127 (1953)
Notes: Which material?

## Slide 15: The microscopic BCS theory
What needed to be explained?
Zero Resistance and Meissner Effect
Coherence (Non-local relation between current density and E-field)
Energy Gap (exponential specific heat)
  Suggests a Bose-Einstein condensation like process
The isotope effect
  The transition temperature of mercury depends on the isotopic mass
  This suggests that the lattice is important for superconductivity

## Slide 16: The microscopic BCS theory
Pairing of electrons close to the Fermi level into Cooper pairs through interaction with the crystal lattice
  Boson (no Pauli exclusion principle)
  All cooper pairs condense to the same ground state
  Coherent wave functions  no scattering  zero resistance
Size of a cooper pair is large compared to the lattice constant and is related to the coherence length ξ
Estimated size of a cooper pair:
Relaxation time of the lattice: 2π/ωD≈10-13s
Electrons move with vF≈106m/s
Distance between electrons forming a cooper pair:
vF≈10-7m

## Slide 17: The microscopic BCS theory
The superconducting state consists of electron pairs and elementary excitations, quasiparticles, behaving almost like free electrons
The energy gap Δ separates the energy levels of elementary excitations from the ground state level. At 0K only the ground state is occupied
Density of elementary excitations. There are no states within the energy gap Δ
Temperature dependence of Δ:
The gap has its full value Δ0 at 0K and vansishes at TC
BCS theory
GL theory
The BCS theory has been derived from perturbation theory – valid only close to 0 K
Close to TC the Ginzburg-Landau theory is valid

## Slide 18: Ginzburg-Landau Theory
Based on Landau's previously-established theory of second-order phase transitions
Free energy, F, of a superconductor near the superconducting transition can be expressed in terms of a complex order parameter
Assuming |ψ| and A and their gradients to be small, the free energy can be expressed in a Taylor series
Extension to include magnetic fields
Energy needed to reduce the external field Ba inside the SC to Bi
Energy change from currents necessary to cause a spatial variation of ψ

## Slide 19: Ginzburg-Landau Theory
A
London equation:
Minimizing gS wrt to Δy and ΔA (variational method) yields the Ginzburg-Landau equations:
Characteristic lengths:
Penetration depth is the length scale for the variation of the magnetic field
Coherence length is the length scale for the variation of the order parameter
Ginzburg-Landau parameter

## Slide 20: DC electrical conduction: resistance
Ohm´s law:
DRUDE MODEL
Kinetic Theory of Gases
Electron scattering time τ. Probability of scattering within time interval dt is dt/τ
After scattering p=0.
+ Free Acceleration between collisions
Average momentum
Probability for scattering within dt
Probability for no scattering within dt
Drude model electrons (shown here in blue) constantly bounce between heavier, stationary crystal ions (shown in red).
Steady state:
Momentum gain of unscattered electrons
The Drude model provides an understanding what conductivity is.
The steady state solution is useful for RF application, where the RF period is much longer than the scattering time.
Only E fields:
Scattering time t = l/vF  10-14s
Notes: Scattering to zero makes sense when a large number of particles is considered. The average momentum is zero if it is treated as a vector.

## Slide 21: Outline
Quick recap of London theory and demonstration of the Meissner effect
Surface Resistance
  Electrodynamics of normal conductors
    Normal and anomalous skin effect
  Electrodynamics of superconductors
    Surface impedance of superconductors in the two fluid model and the BCS theory
    Residual resistance
    Field dependence of surface resistance
Maximum RF field
  DC critical fields, Hc, Hc1, Hc2, Hsh
  Critical field under RF
Materials for SRF
  Why niobium
  Materials beyond niobium
  Multilayers

## Slide 22: Electrodynamics of normal conductors
Maxwell’s equations
(linear and isotropic) material’s equations
j=σE
Hy(x,t)
Ez(x,t)
x
z
y
For a good conductor at RF frequencies, we<<s →
Solution (semi-infinite slab):

## Slide 23: Surface Impedance
The surface impedance is defined as:
surface resistance
surface reactance
For the semi-infinite plane conductor:
Hy(x,t)
Ez(x,t)
x
z
y
Notes: Ratio of electric field at the surface to the total current flowing across a unit line in the surface.
The surface resistance of the semi-infinite plane conductor is the same as the dc resistance of a plane conductor of depth \delta

## Slide 24: Surface resistance: intuitive meaning

Since we will deal a lot with the surface resistance Rs in the following, here is a simple DC model that gives a rough idea of what it means:
Consider a square sheet of metal with resistivity ρ and calculate its resistance to a transverse current flow:
In this model the surface resistance Rs is the resistance that a square piece of conductor opposes to the flow of the currents induced by the RF wave, within a layer 
current
d
a
a
Courtesy: S. Calatroni
Resistance of a square metal sheet of thickness d:
Surface Resistance of a square metal sheet with penetration depth :

## Slide 25: What happens at low temperature?
Surface resistance of Cu at 1.5 GHz as a function of temperature with conductivity σ=1/ρ
At room temperature the conductivity is dominated by phonon scattering
At low temperature phonons “freeze out” and the conductivity depends on impurity concentration.
The residual resistivity ratio RRR = (0K)/(300K) is a measure of material purity
Rs(4.2 K)  1.3 mW
To reduce RS below the mΩ range for RF application we need superconductivity!
Rs=1/sd
Anomalous skin effect l>δ
Courtesy: G. Ciovati
…in spite of the resistivity decreasing by a factor 300 from 300 K to 4.2 K, Rs only decreases by a factor of ~8!
Notes: Less numbers. Better explanation of anomalous skin effect. Some numbers

## Slide 26: The RF surface resistance (intuitive approach)
Consider an alternating magnetic field at the surface of a semi-infinite superconductor
Consider Faraday's law of induction
(t)=Byexp(i
J,E
B
Vacuum
Superconductor
y
x
Integration area

## Slide 27: The RF surface resistance (intuitive approach)
B(x)
Ez and By are both independent of y
Ohms law:
J,E
B
Vacuum
Superconductor
y
x

## Slide 28: The RF surface resistance (intuitive approach)
electron density
temperature (K)
Tc
n
ns
Close to 0 K:
Definition of the
Surface resistance

## Slide 29: Historical Overview
1908 Liquefaction of helium (4.2 K)
1911 Zero resistance
1933 Meissner effect
1935 Phenomenological theory of H. & F. London
1950 Ginzburg – Landau theory
1951 – 2 types of superconductors (Abrikosov)
1957 Bardeen – Cooper – Schrieffer microscopic theory
1960 Magnetic flux quantisation
1962 Josephson effect
1986 High temperature superconductors (Bednorz – Müller)
Bardeen – Cooper – Schrieffer (BCS)
Abrikosov
Ginzburg
Bednorz
Müller
Landau

## Slide 30: Surface Resistance of Superconductors
Superconducting currents are transported by Cooper pairs formed of two electrons
  flow without friction  DC supercurrents are lossless
For temperatures above 0 K not all electrons form Cooper pairs
Cooper pairs have a finite inertia. Under RF fields a time-varying E-field is induced in the material. Normal electrons see this field, move and dissipate
Rs > 0
+
j=σE
+

## Slide 31: Surface Resistance in the two fluid model
Basic ingredients for RF superconductivity
  Two fluid model (Gorter-Casimir)
  Maxwell electrodynamics
  London equations
electron density
temperature (K)
Tc
n
ns
Basic assumptions of two fluid model
  all free electrons of the superconductor are divided into two groups:
    superconducting electrons of density ns
    normal electrons of density nn
  The total density of the free electrons is
  n = ns + nn
  As the temperature increases from 0 to Tc, the density ns decreases from n to 0.

## Slide 32: Surface Resistance in the two fluid model
Electrodynamics of sc is the same as nc, only that we have to change s  s1 – i s2
= s2
s
Penetration depth:
s1 << s2 for sc at T<<Tc
Interesting to note here: -We have derived λL from DC arguments before
- Now we find δ=λL for T<<Tc
London equation:
Two fluid model:
Scattering time t = l/vF  10-14s
Notes: E=Eeiwt… Rework!!!

## Slide 33: Surface Resistance in the two fluid model
Hy(x,t)
Ez(x,t)
x
z
y
+i
Electrodynamics of sc is the same as nc, only that we have to change s  s1 + i s2
Recall the definition of the surface impedance:
For σ1<< σ2 we obtain:
Ls: kinetic inductance

## Slide 34: Rs within BCS theory
Mattis and Bardeen (1958) used time dependent perturbation theory to derive RS for weak RF fields
Within this theory no simple formula can be derived. Several approximate formula can be found in the literature for some limits. For example for the dirty limit
There are numerical codes (Halbritter (1970) to calculate RBCS as a function of w, T and material parameters (x0, lL, Tc, D, l)
For example, http://www.lepp.cornell.edu/~liepe/webpage/researchsrimp.html
/T

## Slide 35: Rs within BCS theory
Be carefureful here. The website suggests 40nm. The input required is πξ0/2, while ξ0≈40nm for Nb

## Slide 36: BCS vs two fluid model
The treatment within BCS theory and two-fluid model give qualitatively similar results
Quantitatively they can differ by an order of magnitude
  The BCS treatment gives qualitatively correct results for low field
To treat experimental data approximate formulae are useful, e.g.
Here A accounts for all material parameters

## Slide 37: The RF surface resistance
This equation implies RS:
Has a minimum for medium purity
Is proportional to
Decreases exponentially with temperature
Vanishes as T0 K
Is independent of RF field strength
In the following we will compare these assumptions to experimental data and modify the formula if necessary

## Slide 38: Material purity dependence of Rs
The dependence of the penetration depth on l is approximated as
s1  l
if l >> x0 (“clean” limit)
if l << x0 (“dirty” limit)
Rs has a minimum for l = πx0/4
C. Benvenuti et al., Physica C 316 (1999) 153.
Nb on Cu,1.5 GHz, 4.2 K
“clean”
“dirty”
Example: Nb films sputtered on Cu substrate
By changing the sputtering species, the mean free path was varied
RRR of niobium on copper cavities can be tuned for lowest RS.

## Slide 39: CERN – Nb on Cu cavities
CERN first started to use Nb on Cu technology for LEP-II cavities.
Du to the low frequency and optimal mean free path economical operation at 4.5K was possible
Hie-Isolde cavities
LHC cavities
352 MHz
400 MHz
100 MHz
The technology was then adopted for the 400 MHz LHC cavities
Hie-Isolde Quarter Wave Resonator commissioned in 2015

## Slide 40: The RF surface resistance
This equation implies RS:
Has a minimum for medium purity
Is proportional to
Decreases exponentially with temperature
Vanishes as T0 K
Is independent of RF field strength
In the following we will compare these assumptions to experimental data

## Slide 41: The RF surface resistance
Normal Conducting
Superconducting
400MHz
800MHz
1200MHz
(T)+Rres
Measurement of the surface resistance at low field of niobium at three frequencies with the Quadrupole Resonator

## Slide 42: The RF surface resistance
This equation implies RS:
Has a minimum for medium purity
Is proportional to ( )
Decreases exponentially with temperature
Vanishes as T0 K
Is independent of RF field strength
+Rres

## Slide 43: The residual resistance
According to the BCS theory there are no quasiparticle states within the energy gap Δ
Smearing of Density of States leads to a residual resistance
Point contact tunneling experiments on Nb and Nb3Sn have found finite density of states (DOS) inside the energy gap
T. Proslier et at Appl Phys Lett 92 212505 2008
Subgap states will yield a finite RS(0K) irrespective of physical mechanism

## Slide 44: The residual resistance
DoS smearing is not the only cause of residual resistance
Other contributions to Rres:
Trapped magnetic flux and thermal currents
Lossy oxides, metallic hydrides
Normal conducting precipitates
Grain Boundaries
Interface Losses
Magnetic Impurities

## Slide 45: Trapped Magnetic Flux
Well understood contribution to Rres
When a cavity is cooled down in an ambient DC magnetic field not all flux is expelled – Incomplete Meissner effect
In fact fields of a few µT (order earth magnetic field) can be completely trapped
In cryomodules thermal currents can cause additional magnetic fields which can be trapped

## Slide 46: Trapped Magnetic Flux
for RRR=300
H. Padamsee et al. RF Superconductivity for Accelerators
Simple model with these assumptions:
  Fluxoids are perpendicular to the cavity surface
  Fluxoids are static, no displacement due to RF fields
  RF currents flow around them
  Flux completely trapped
  Losses are independent on RF field
Additional residual resistance=Ratio nc/sc areaNormal conducting surface resistance

## Slide 47: The RF surface resistance
This equation implies RS:
Has a minimum for medium purity
Is proportional to ( )
Decreases exponentially with temperature
Vanishes as T0 K
Is independent of RF field strength
+Rres

## Slide 48: Surface treatments for State of the art SRF cavities
Maximum quality factor and accelerating gradient depend on surface treatment but also on RF frequency, cavity shape (surface field configuration), ambient magnetic flux in a correlated and not fully understood way

## Slide 49: The RF surface resistance
This equation implies RS:
Has a minimum for medium purity
Is proportional to ( )
Decreases exponentially with temperature
Vanishes as T0 K
Is independent of RF field strength
+Rres
Not only do RBCS and Rres depend on the RF field strength there can also be additional extrinsic losses limiting the cavity performance

## Slide 50: Field emission
Under high RF fields electrons can be released from the surface and accelerated.
Released electrons will impact on the cavity wall creating x-rays and heating  Reduced Q-value
Field emitters found on dissected cavities (size 0.5-10μm with sharp edges)

## Slide 51: Field emission
Solution to field emission – high pressure water rinsing (100 atm), and an ultra-clean assembly => remove field emitters and preserve cleanliness
A lot more on this in Ari’s lecture tomorrow

## Slide 52: Thermal Breakdown
Quench is the final limitation set by the critical field of the material
A quench can however occur at much lower fields if the magnetic field locally exceeds the critical field or the temperature exceeds the critical temperature at sub mm size defects of high resistivity
At high fields these defects will heat up its surrounding area above Tc and a normal conducting area will spread causing a quench
Avoiding thermal breakdown
Use material with high thermal conductivity: high purity niobium or niobium on copper cavities
Careful electron beam welding
Post processing
In production usually the cavity is chemically etched again
Big defects with sizes of 1 mm can be mechanically grinded away. This requires knowledge of the quench position from online diagnostics during cold test and optical inspection afterwards.

## Slide 53: Quench localization and visualization
Quench sites can be located with temperature mapping
Afterwards the location can be visualized with an optical inspection system
Alternative approaches to temperature mapping are
Second sound – Y. Tamashevich
Transition Edge Sensors – H. Furci (both talks on Thursady)

## Slide 54: Performance of SRF cavities
There are two parameters which define the performance of an SRF cavity: Quality factor and the accelerating gradient
B
E
The quality factor. Remember:
Q0 =G/RS=U/Ploss
The accelerating gradient can be limited by the peak surface electric field (field emission) or the peak surface magnetic field (quench)
Eacc ∝ Bpeak
Intrinsic limitations: Q-disease and Q-slope

## Slide 55: The hydrogen Q-disease
If a cavity is cooled down slowly around 50-150K Q decreases
Effect correlated to hydrides
Some cavities recover after warm up to RT
800C baking is always effective

## Slide 56: Performance of SRF cavities
There are two parameters which define the performance of an SRF cavity: Quality factor and the accelerating gradient
B
E
The quality factor. Remember:
Q0 =G/ RS=U/Ploss
The accelerating gradient can be limited by the peak surface electric field (field emission) or the peak surface magnetic field (quench)
Eacc ∝ Bpeak
lntrinsic limitations: Q-disease and Q-slope

## Slide 57: The high field Q-slope
Observations:
    Strong decrease of Q0 above Eacc > 20 MV/m
    Tesla cavities( Bp > 85 mT )
    Field emission not involved ( no e -, no X rays )
    T map : global heating in the area of max B-field
    Limitation by RF power supply or quench
    Seemingly a typical feature of BCP cavities
“European Headache”
superiority of EP
without Q-slope
( E. Kako et al. - SRF ’99 - Santa Fe )
( L. Lilje et al. - SRF ’99 - Santa Fe )
K. Saito et al.
SRF ’97
( Abano Terme )
( Nb 1-cell cavity )

## Slide 58: Baking Effect on BCP Cavities
    “in-situ” baking discovered on BCP cavity
  slope improvement ( 90 < T < 120°C ) - degradation ( T > 150°C )
( B. Visentin et al. – EPAC ’1998 - Stockholm )
Baking reduces RBCS but increases Rres:

## Slide 59: Baking Effect on EP Cavities
Courtesy B. Visentin
  Same phenomenon on E.P. cavities
  before baking: Q-slope identical to BCP
      after baking : Q-slope improvement
apparent superiority of EP reported before ?
cleaning procedure at KEK
wet cavities ( High Power Rinsing )
directly pumped out and baked at 85°C/20h
to accelerate pumping speed
( Saclay cavity – EP & tested @ KEK )
P. Kneisel. – TUP 044
K. Saïto. – TUP 031
L. Lilje et al. – TUA 001
B. Visentin et al. – TUP 015
SRF ’ 99
Santa Fe

## Slide 60: Field dependence of Rs
Strong RF currents affect superconducting properties, in particular the DOS
Observed normal ΔRS/ΔB>0 mainly due to external sources and dependent on material preparation
Inversed ΔRS/ΔB <0 is thought to be intrinsic
A theory of non-linear RS at high field [A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)]
Rs(H) was re-derived from first principles (BCS) taking into account oscillations of N(e, t) due to RF current pairbreaking and non-equilibrium distribution function of quasiparticles in the dirty limit
Left: σ1 calculated for different levels of quasiparticle overheating parametrized by α. Right: Nb cavity at 1.75 GHz fitted with α=0.91

## Slide 61: Surface treatments for State of the art SRF cavities
Maximum quality factor and accelerating gradient depend on surface treatment but also on RF frequency, cavity shape (surface field configuration), ambient magnetic flux in a correlated and not fully understood way
Nb is reaching fundamental limits in quality factor and accelerating gradient.
Unfortunately so far we can have only one or the other and only for elliptical niobium cavities.
There is still margin for improvement of non-elliptical cavities.
For performance far beyond the state of the art of elliptical cavities materials other than Nb need to considered
Are these fundamental limit?

## Slide 63: Outline
Quick recap of London theory and demonstration of the Meissner effect
Surface Resistance
  Electrodynamics of normal conductors
    Normal and anomalous skin effect
  Electrodynamics of superconductors
    Surface impedance of superconductors in the two fluid model and the BCS theory
    Residual resistance
    Field dependence of surface resistance
Maximum RF field
  DC critical fields, Hc, Hc1, Hc2, Hsh
  Critical field under RF
Materials for SRF
  Why niobium
  Materials beyond niobium
  Multilayers

## Slide 64: Energy balance at a SC-NC interface
s.c
Vacuum/n.c
Energy loss:
The density of cooper pairs is suppressed over the distance
Energy gain:
Field does not need to be expelled over the distance
z
x
l
y
B
If it is energetically favourable to create normal-superconducting boundaries above the lower critical field Bc1
These superconductors are referred to as type-II
: Energy difference at a NC-SC boundary compared to the SC state
Bc: crtical thermodynamic field, above Bc the normal conducting state is energetically favorable
=0 and resolve wrt B
Exact result from GL theory
Notes: Give real GL result

## Slide 65: Two types of superconductors
Type II Superconductors
  Impure metals including high RRR niobium as used for SRF cavities
  All alloys
  For >>1 local electrodynamics (London theory) applicable
Type I Superconductors
  All elements including very pure niobium Phys. Rev. B 106, L180505 (2022)
  Non-local electrodynamics needs to be considered

## Slide 66: Flux Quantization
Deaver und Fairbank
Magnetic flux
Applied Field
It is energetically favorable for Type-II superconductors to create normal superconducting boundaries
The energy is minimized if the boundary area is maximized
However quantum mechanics does not allow for infinite small domains
  This leads to flux quantization

## Slide 67: Flux Quantization
In Type-II superconductors flux tubes are created each carrying one flux quantum (the minimal flux allowed by quantum mechanics)
Flux tubes are repulsive creating therefore the vortex lattice
STM image of Vortex lattice, 1989
H. F. Hess et al. Phys. Rev. Lett. 62, 214 (1989)

## Slide 68: The Magnetization Curve
Under DC fields flux tubes can be pinned – no dissipation
    SC magnets are operated between Hc1 and Hc2
Under RF fields flux tubes oscillate – dissipation
  RF cavities are operated in the Meissner state
Can the Meissner state persist metastable beyond Hc1?
Cavities
Magnets

## Slide 69: The superheating field
The superheating field Hsh is set by the competition between magnetic pressure (imposed by the external magnetic field), the energy cost to destroy superconductivity, and the attractive force due to the zero-current boundary condition at the interface.
Hc1 is the field where it is energetically favourable for the flux to be in the superconductor
Hsh is the field where the Bean-Livingston barrier for flux entry disappears
Defects can serve as entry points for flux preventing superheating
Suggested further reading:
B. Liarte et al. - Supercond. Sci. Technol. 30 (2017) 033002

## Slide 70: The superheating field
Niobium:
  Close to Tc Hentry=Hsh
  T<<Tc usually Hentry<Hsh
Nb3Sn:
  Close to Tc Hentry=Hsh
  T<<Tc Hentry<<Hsh
RF heating proportional to H2. Close to Tc less power is dissipated. Flux entry less likely.
Coherence length of Nb3Sn smaller than Nb. Flux entry at defects more likely.
The good news is Hc1 is not a general limitation!
S. Posen et al. PRL 115, 047001 (2015)

## Slide 71: Outline
Quick recap of London theory and demonstration of the Meissner effect
Surface Resistance
  Electrodynamics of normal conductors
    Normal and anomalous skin effect
  Electrodynamics of superconductors
    Surface impedance of superconductors in the two fluid model and the BCS theory
    Residual resistance
    Field dependence of surface resistance
Maximum RF field
  DC critical fields, Hc, Hc1, Hc2, Hsh
  Critical field under RF
Materials for SRF
  Why niobium
  Materials beyond niobium
  Multilayers

## Slide 72: Nb3Sn
Nb3Sn can have the same Rs at 4.2K as Nb 2K as ΔTc

## Slide 73: Multilayer
A. Gurevich - Supercond. Sci. Technol. 30 (2017) 034004
To address the low-Bc1 problem of high-Bc materials, it was proposed to coat the Nb cavities with multilayers of thin superconductors (S) separated by dielectric (I) layers
For dS<λ no thermodynamically stable parallel vortices in decoupled S layers

## Slide 74: SRF Material of the future

## Slide 75: Recommanded Literature
General solid state physics
S.H Simon The Oxford Solid State BasicsGeneral, OUP Oxford, 2013
General Superconductivity
W. Buckel and R. Kleiner, « Superconductivity: Fundamentals and applications», Wiley-VCH 2004
V. V. Schmidt « The physics of superconductors », Springer 1997
M. Tinkham, « Introduction to superconductivity », McGraw-Hill 1996
Online lectures from Cambridge University: http://www.msm.cam.ac.uk/ascg/lectures/fundamentals/isotope.php
RF Superconductivity
R. Padamsee, J. Knobloch and T. Hays – « RF Superconductivity for Accelerators », Wiley-VCH, 2008
J. P. Turneaure, J. Halbritter, and H. A. Schwettman. « The surface impedance of superconductors and normal conductors: The Mattis-Bardeen theory. » Journal of Superconductivity 4.5 (1991): 341-355.
A. Gurevich « Theory of RF superconductivity for resonant cavities. » Superconductor Science and Technology, 30(3), 034004 (2017).
A. Gurevich «Tuning microwave losses in superconducting resonators. »
Supercond. Sci. Technol. 36 063002 (2023)
SRF23 Tutorial A. Miyazaki

## Slide 76: Thank you
Questions?